## Slide 1
First-principles calculations of opto-electronic and thermoelectric properties double perovskite semiconductors M2ScInCl6 (M = Rb, Cs)
Mohammad Abdur Rashid
Md. Borhanul Asfia, Sahadat Jaman

## Slide 2
Outline
Lead-free double perovskite
Our systems of study: Rb2ScInCl6 and Cs2ScInCl6
Computational details
Opto-electronic properties
Thermoelectric properties
Conclusions

## Slide 3
Perovskite solar cells
High power conversion efficiency (about 25%)
Easier manufacturing process
Lower cost and greater flexibility
Perovskites degrade much faster
Pb-based perovskites show better
potential but they are toxic
https://news.mit.edu/2022/perovskites-solar-cells-explained-0715

## Slide 4
Environmental sources of lead exposure
https://www.cdc.gov/nceh/lead/publications/refugeetoolkit/powerpoint_files/medicalservice.ppt

## Slide 5
Lead-free double perovskites: A2B+B3+X6
https://pubs.acs.org/doi/10.1021/acsenergylett.6b00499

## Slide 6
Structure of M2ScInCl6 (M = Rb, Cs)
M
In
Sc
Cl

## Slide 7
Computational details
RMT(Cs, In) = 2.50 a.u.
RMT (Rb, Sc) = 2.35 a.u.
RMT (Cl) = 1.15 a.u.
RMT×Kmax = 8.0
K-mesh = 10×10×10
EC = 0.00001 Ry & CC = 0.0001 e

## Slide 8
Optimized Lattice parameters

## Slide 9
Optimized Lattice parameters
System | Lattice parameter (Å) | Band gap (eV) | 
 |  | PBE-GGA | TB-mBJ
Rb2ScInCl6 | 11.073 | 2.599 | 2.662
Cs2ScInCl6 | 11.163 | 2.802 | 2.902

## Slide 10
Electronic properties

## Slide 11
Electronic properties

## Slide 12
Optical properties

## Slide 13
Optical properties

## Slide 14
Optical properties

## Slide 15
Thermoelectric properties

## Slide 16
Thermoelectric properties

## Slide 17
Conclusions
Opto-electronic and thermoelectric properties double perovskites M2ScInCl6 (M=Rb, Cs) using WIEN2k
Both compounds show semiconductor like behavior
Remarkable optical properties
Good Seebeck coefficient and power factor
Promising materials for different opto-electronic and thermoelectric applications